TECHNICAL DATA SHEET 
Iron Oxide Black 780
	Appearance 
	Black pigment 

	Delivery Form 
	Powder 

	Chemical Class 
	Synthetic iron oxide Fe3O4 

	Color Index 
	Pigment Black 11 (77499) 

	CAS No． 
	1317-61-9

	Use Recommendation 
	Coatings, Construction, plastic, Rubber, etc


	TECHNICAL DATA 

	Item 
	Specification 
	Test Method 

	Color  Shade（△E）max
	1.0 
	----------------------------

	Tinting Strength %
	95-105
	----------------------------

	Water-Soluble Content [%] Max
	0.5 
	DIN EN ISO787 Part 3 (1995) 

	Sieve Residue（0.045mm）[%] Max
	0.4 
	DIN EN ISO787 Part 2 (1995) 

	PH Value 
	4.0 ----8.0 
	DIN EN ISO787 Part 9 (1995) 

	Fe3O4 [%]  min
	92.0   
	DIN 55913 Sheet 2 (1972) 

	Moisture (After Production) [%]  Max
	1.0 
	DIN EN ISO 787 Part 2 (1995)

	Oil Absorption [g/100g] 
	15-25 
	DIN EN ISO787 Part 5 (1995) 


	STANDARD PACKAGING 
	25kg/bag with pallet, wrapped and shrinked

1000kgs/1100kgs jumbo bags with pallet 

	TRANSPORT AND STORAGE 

	Protect against weathering. Store in a dry place and avoid extreme fluctuations in temperature. Special conditions for opened packaging: Close bags after use to prevent the absorption of moisture and contamination. 

	SAFETY 

	The product is not classified as dangerous under the relevant EC directives and corresponding national regulations valid in the individual EU member states. It is not dangerous according to transport regulations. In countries outside the EU, compliance with the respective national legislation concerning the classification, packaging, labeling and transport of dangerous substances must be ensured. 

The information contained in the safety data sheet should be observed. 

This contains information on handing, product safety and ecology. 


This information is given in good faith, without warranty. It is also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to verify the information currently provided and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General conditions of sale and delivery. 
